# Text boxes

JRC16N1659

This is to certify that the nominated size and quality of the following AMG product has been manufactured, inspected and tested to conform to 5467 with the following results.

Certificate No:

60.0Kn

122.1Kn

SIZE

| D | L | B | b |
| --- | --- | --- | --- |
| mm | mm | mm | mm |
| 10.0 | 65.0 |  | 20.0 |

Description:

Rating Capacity:

Proof Load:

Manufactured, Inspected and Tested for and on behalf of:

Allan Marketing Group

42 Clements Avenue Bundoora Australia

Authorised Signatory

Date:

Breaking Load:

RUD-161010HESNZ

Trailer Chain HDG G70 Long Link 10mm

NZS5467

Batch Number:

3500kg MTM

CHEMICAL COMPOSITION

| C | Si | Mn | P | S | Cr | Ni | MO |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0.20 |  |  | 0.17 | 0.003 |  |  |  |

10/04/2015 – PO1757

20.0%

Elongation:

MILL/TEST CERTIFICATE